CHAPTER

Carbon Materials for Electrochemical Biomass Conversion

Jagadeeswari Rangaraman, Nishanth. M, Logith A K, Keerthi Kumar K J, G. Kausalya Sasikumar

1Department of Chemistry, KPR Institute of Engineering and Technology, Coimbatore -641407, Tamil Nadu India.

2,3,4Department of Electronics and Communication Engineering, KPR Institute of Engineering and Technology, Coimbatore -641407, Tamil Nadu India.

*Centre of Research and Development,KPR Institute of Engineering and Technology,Coimbatore 641407,Tamil Nadu, India.

Email: kausalyasasikumar91@gmail.com*

Abstract:

Electrochemical biomass conversion is a sustainable pathway to transform renewable biomass into value-added chemicals, fuels, and advanced materials. Carbon materials, including graphene, biochar, and hybrid nanostructures, play a crucial role as catalysts or conductive supports due to their high conductivity, large surface area, and tunable functionalities. Advances in synthesis and functionalization have enhanced catalytic efficiency and selectivity, enabling processes like glycerol oxidation and CO₂ reduction under mild conditions. Challenges remain in material durability, scalability, and process economics. Emerging trends involve AI-driven catalyst design and integration with renewable energy, positioning carbon-based electrochemical technologies as vital solutions for sustainable chemical production and carbon neutrality goals.

Keywords:

Carbon materials, electrochemical biomass conversion, biochar, electrocatalysis, glycerol oxidation, CO₂ reduction.

1 Introduction

Carbon materials play a pivotal role in the electrochemical conversion of biomass, a process that transforms renewable organic resources into value-added chemicals, fuels, and materials. Derived from various biomass sources, these carbon materials exhibit unique properties, such as high electrical conductivity, large specific surface area, tunable porosity, and chemical stability. These characteristics make them ideal candidates for applications in energy storage, electrocatalysis, and sustainable chemical production.

The electrochemical conversion process relies on carbon-based electrodes to facilitate oxidation and reduction reactions of biomass-derived compounds. Advances in material science have enabled the development of biomass-derived carbon with enhanced performance through innovative synthesis strategies, such as templating, activation, and doping with heteroatoms. These modifications improve catalytic activity, charge transfer efficiency, and durability under operational conditions.[28]

The growing interest in this field is driven by the need for sustainable and cost-effective solutions to replace fossil-based technologies while contributing to carbon neutrality. However, challenges remain, including the scalability of production methods, maintaining uniform material properties, and optimizing reaction mechanisms for broader industrial applications [21] [22].

1.1 Overview of Electrochemical Biomass Conversion

Electrochemical biomass conversion involves transforming organic compounds derived from biomass into value-added chemicals, fuels, or energy using electrochemical methods. This approach leverages renewable electricity and often operates at low temperatures and pressures, providing a more sustainable alternative to traditional thermochemical processes. Techniques such as electrocatalysis, microbial electrolysis, and bioelectrosynthesis are utilized to target specific intermediates for upgrading, offering high efficiency and adaptability for renewable energy integration [18] [20].

1.2 Role of Carbon Materials in Biomass Electro conversion

Carbon materials play a critical role in biomass electroconversion, acting as electrode supports or catalysts. Their properties—such as high electrical conductivity, chemical stability, and surface area—facilitate efficient electron transfer during redox reactions. Functionalized carbon materials, including graphene and carbon nanotubes, improve catalytic performance and enable selective reactions, such as hydrogen evolution or oxygen reduction, vital for biomass valorization [18] [19].

Figure 1 Two half-cells (anode and cathode) connected via a salt bridge, with ions flowing through the bridge and electrons through an external circuit—typical of galvanic/electrolytic systems.
(CC BY SA 3.0; adapted from Cmx, 2005; license details in ref.)

2 Fundamentals of Electrochemical Biomass Conversion

2.1 Redox Reactions and Electrocatalysis in Biomass Transformation

Redox reactions form the backbone of electrochemical biomass transformation, where electron transfer drives the breakdown or synthesis of organic compounds. Electrocatalysts—often metal-based or supported on carbon—are essential to lowering the activation energy for these reactions, improving efficiency. For example, nickel and palladium catalysts are employed for hydrogenation and deoxygenation processes, enabling the selective transformation of lignocellulosic feedstocks into biofuels and specialty chemicals [18] [19][29].

2.2 Electrochemical Cell Configurations for Biomass Valorization

Electrochemical cells used for biomass valorization include configurations such as microbial fuel cells (MFCs) and proton-exchange membrane cells. MFCs convert organic biomass into electricity using microorganisms, while other systems focus on the electrocatalytic upgrading of biomass intermediates like lignin. These setups are optimized for high efficiency, low energy input, and minimal environmental impact. Advanced designs incorporate flow-through architectures to reduce mass-transfer limitations and enhance scalability [20] [19].

3 Challenges in Electrochemical Biomass Valorization

3.1 Selectivity and Efficiency in Biomass-Derived Reactions

Achieving high selectivity and efficiency in biomass conversion is challenging due to the complexity of biomass feedstocks and their multifunctional chemical structures. Controlling reaction pathways to minimize side products and ensure target chemical production is key. Factors such as catalyst design and process optimization play significant roles [23].

3.2 Material Stability and Scalability of Carbon Catalysts

The durability and scalability of carbon-based catalysts for biomass electroconversion are critical for industrial applications. Challenges include ensuring long-term stability under harsh conditions and developing cost-effective synthesis methods for large-scale use [23][29].

Figure 2 Classification of carbon materials including graphene, carbon nanotubes, biochar, activated/carbon black—with clear representation of micro- and nanostructures.
(CC BY 4.0; adapted from Vinay Bhat, 2019; license details in ref.)

4 Carbon Materials for Biomass Conversion

4.1 Types of Carbon Materials for Biomass Applications

4.1.1 Graphene and Doped Graphenes: These materials offer high conductivity and surface area, enhancing catalytic activity. Doping with elements like nitrogen improves functional group interactions [23]

4.1.2 Biomass-Derived Carbons: Materials like biochar and hydrochars are sustainable and versatile, derived directly from biomass waste [23]

4.1.3 Hybrid Carbon Materials with Functional Groups: These materials combine carbon with functional additives, enhancing selectivity and stability [23]

4.2 Synthesis and Functionalization of Carbon Catalysts

Advanced synthesis techniques enable precise control over carbon structures, tailoring porosity, and surface chemistry for specific reactions. Functionalization, such as incorporating heteroatoms, improves catalytic efficiency [23].

4.3 Key Properties of Carbon Materials for Biomass Electroconversion

Important properties include electrical conductivity, stability under reaction conditions, and compatibility with biomass substrates. Tailored properties enhance reaction selectivity and efficiency, optimizing biomass valorization [23][31].

5 Electrochemical Valorization of Biomass Using Carbon Materials

Valorisation of biomass refers to the process of transforming low-value or waste biomass into higher-value products, such as chemicals, materials, or fuels. Key Valorization Pathways includes generally the oxidation and reduction reactions of Biomass.

5.1 Oxidation Pathways for Biomass-Derived Molecules

Electrochemical oxidation of biomass-derived intermediates is a sustainable approach to producing high-value chemicals. Over the last 60 years, glycerol (1,2,3-propanetriol) has transitioned from a scarce industrial chemical to a byproduct produced in excess during biodiesel manufacturing. Recent improvements in its usage and conversion into value-added chemicals emphasize glycerol's importance as a crucial raw material in future biorefineries. [4] Another critical pathway is the conversion of 5-hydroxymethylfurfural (5-HMF), a platform chemical derived from lignocellulosic sugars, into 2,5-furandicarboxylic acid (FDCA).

5.1.1 Glycerol to Lactic Acid

Glycerol, a byproduct of biodiesel production, is an abundant biomass derivative with potential for electrochemical valorization. In this case study, activated carbon-supported CuO catalysts were prepared by an ammonia evaporation method and applied to catalyze the selective oxidation of glycerol to lactic acid. The effects of CuO loadings on the structure and catalytic performance of the catalyst were investigated. Results showed that CuO could be dispersed uniformly on the surface of activated carbon, promoting the increase of the reaction rate, and accelerating the glycerol conversion significantly.[5] This pathway offers a sustainable method for lactic acid production, critical for bioplastics and pharmaceutical applications.

5.1.2 5-HMF to FDCA

The conversion of 5-hydroxymethylfurfural (5-HMF) to 2,5-furandicarboxylic acid (FDCA) via electrochemical oxidation is a critical process in biomass valorization. FDCA is a sustainable alternative to terephthalic acid, a key monomer in traditional plastics, and is essential for producing bio-based polyethylene furanoate (PEF), which offers superior barrier properties and recyclability compared to polyethylene terephthalate (PET).

Mechanism and Catalyst Innovation

The process involves the selective oxidation of the aldehyde and hydroxymethyl groups in 5-HMF to carboxylic groups. Recent research highlights the role of advanced carbon-based electrocatalysts in this transformation:

- Bio-inspired Catalysts: A manganese-nickel layered double hydroxide (NiMn-LDH) catalyst, inspired by the oxygen-evolving complex in photosynthesis, achieved a remarkable faradaic efficiency of 97% and an FDCA yield of 94.72% under mild electrochemical conditions. The catalyst's active sites enable efficient oxidation while minimizing energy consumption [6].

- Carbon-Encapsulated Metal Nanocrystals: Platelike nickel nanocrystals encapsulated in carbon structures demonstrated a 100% conversion rate of 5-HMF and a 97.4% faradaic efficiency for FDCA production. The encapsulated carbon layer enhances conductivity and stabilizes the catalyst during the reaction, providing industrial scalability [7].

Advantages of Electrochemical Oxidation

- Sustainability: The process operates under mild temperatures and pressures, reducing the need for energy-intensive methods or harsh chemical oxidants.

- Selectivity: Functionalized catalysts enhance product selectivity, ensuring minimal side reactions.

- Industrial Relevance: Companies like Avantium are scaling FDCA production using renewable feedstocks like 5-HMF, highlighting the commercial potential of this technology [8].

Future Perspectives

To improve industrial adoption, researchers are focusing on designing more durable and cost-effective catalysts, integrating renewable energy into the process, and optimizing reactor designs to maximize scalability.

5.2 Reduction Pathways for Biomass Byproducts

5.2.1 CO2 Reduction to Formic Acid or Methanol

The electrochemical reduction of CO2, often a byproduct of biomass processing, provides a sustainable pathway for converting waste gases into valuable chemicals like formic acid and methanol. Biochar and other biomass-derived carbon materials, functionalized with nitrogen or transition metals, are highly effective catalysts for CO2​ reduction due to their ability to stabilize intermediates and lower activation energy. Recent advances demonstrate faradaic efficiencies exceeding 90% for formic acid production under mild conditions. Methanol synthesis, involving multi-electron reductions, has also been enhanced by using hierarchically porous carbon materials, which provide improved CO2 adsorption and reaction kinetics. The process is further augmented by coupling with renewable electricity sources like solar or wind, aligning with carbon-neutral goals [9][11]

5.2.2 Biomass Pyrolysis Products to Fuels

Biomass pyrolysis generates bio-oil, biochar, and syngas, all of which can be upgraded into renewable fuels. Bio-oil, rich in oxygenated hydrocarbons, undergoes electrochemical reforming to produce hydrogen, methane, or ethanol. Advanced carbon-based electrodes, including biochar derived from agricultural residues, facilitate these conversions by providing high conductivity and stability. For example, Kore Infrastructure has developed modular pyrolysis systems that convert bio-oil and syngas into vehicle-grade hydrogen and renewable natural gas (RNG). This approach integrates seamlessly with decentralized renewable energy systems, achieving carbon-negative outcomes while generating usable fuels. [9] [11]

In addition, biochar-based electrodes support hydrogen evolution reactions (HER) during bio-oil electrolysis, achieving high selectivity and energy efficiency. These technologies not only valorize biomass pyrolysis products but also contribute to waste minimization and carbon sequestration.

[10] [11]

Figure 3 Main synthesis methods for preparing biomass-derived carbon materials for sensing applications.

(CC BY 4.0; adapted from Onfray, C. Thiam, A., 2023; license details in ref.)

6. Case Studies in Biomass Electrochemical Conversion

6.1 Industrial-Scale Biomass Conversion Systems

Electrochemical biomass conversion technologies are scaling up to industrial applications, leveraging advanced tools such as computational modeling to optimize processes. For instance, researchers at the National Renewable Energy Laboratory (NREL) have developed virtual biorefineries that simulate biomass conversion systems from feedstock to final products. These models help de-risk industrial operations by predicting mechanical failures and optimizing process parameters, such as oxygen distribution in reactors, for efficient fuel production. A prominent example is the scale-up of 2,3-butanediol (BDO) production from biomass-derived sugars using computational fluid dynamics to enhance yields by 25% in microaerated bioreactors. These systems have been integrated with modular pyrolysis setups, enabling flexible deployment across diverse feedstocks like corn stover and pine residues, which are processed into sustainable aviation fuels and renewable chemicals [12] [14]

6.2 Comparative Performance of Carbon Catalysts in Valorization

The performance of various carbon-based catalysts in biomass valorization processes has been extensively studied. A recent comparative analysis highlights the efficiency of nitrogen-doped graphene and hierarchical biochar in catalyzing biomass-derived molecule transformations. Nitrogen-doped graphene exhibits high selectivity for glycerol oxidation to lactic acid, achieving faradaic efficiencies above 85%. Meanwhile, biochar derived from lignocellulosic residues demonstrates superior stability in hydrogen evolution reactions (HER), outperforming traditional metal-based electrodes in energy efficiency and cost-effectiveness. Computationally designed carbon catalysts, such as those integrated with transition metals, have further improved reaction kinetics and product yields, particularly for the conversion of bio-oil into hydrogen and methane. [13] [14]

6.3 Sustainable Hydrogen Production from Bio-Oil Electrolysis

Hydrogen production through bio-oil electrolysis represents a breakthrough in integrating biomass with electrochemical systems for green energy. Bio-oil, derived from biomass pyrolysis, is an oxygen-rich feedstock that undergoes efficient electrochemical reforming to produce hydrogen. Advanced biochar-based electrodes, functionalized with heteroatoms like nitrogen or sulfur, have been shown to enhance faradaic efficiency and hydrogen yield. Recent advancements have achieved nearly 90% faradaic efficiency and high stability under alkaline conditions. This approach also enables carbon sequestration, as residual biochar from pyrolysis can act as a carbon sink. Pilot projects integrating renewable energy sources, such as solar and wind, with bio-oil electrolysis systems have demonstrated promising scalability and economic viability, offering a sustainable alternative to traditional hydrogen production methods [24] [25]

6.4 Biomass-Derived Carbons in Lithium-Ion Batteries

Biomass-derived carbon materials (BDCMs) are emerging as revolutionary components in lithium-ion batteries (LIBs), enabling sustainable energy storage solutions. These materials, synthesized from agricultural residues and lignocellulosic biomass, are used as anode and cathode materials due to their tunable porous structures, high conductivity, and chemical stability. For example, biochar-based electrodes have shown exceptional performance metrics, with initial Coulombic efficiencies exceeding 90% and energy densities approaching 300 Wh/kg. Studies reveal that the microstructure of biomass-derived carbon, such as layered or fibrous forms, significantly impacts the electrochemical performance of LIBs. Advanced fabrication methods, including pyrolysis and templating techniques, have been employed to optimize these structures. This application not only valorizes biomass waste but also contributes to reducing the carbon footprint of battery manufacturing, aligning with global sustainability goals [26] [27].

7 Future Trends in Biomass Electroconversion

7.1 AI-Guided Catalyst Design for Biomass Applications

Artificial Intelligence (AI) is revolutionizing catalyst design for biomass electroconversion, allowing rapid optimization of material properties and reaction conditions. Recent advancements integrate AI workflows that utilize machine learning (ML), Bayesian optimization, and high-throughput experimental data to predict the most effective catalyst configurations. For example, studies employing multi-objective optimization algorithms have identified optimal compositions of catalysts like Co-Mn-Ti oxides for oxygen evolution reactions, achieving a 17-fold acceleration in discovery compared to traditional methods. These approaches significantly reduce trial-and-error experimentation, enabling the customization of carbon-based electrocatalysts for specific biomass valorization reactions, such as glycerol oxidation or CO2_22​ reduction. [15] [17]

Further developments involve integrating AI with large language models (LLMs) to analyze scientific literature and experimental datasets, extracting actionable parameters for designing tailored catalysts. This combination streamlines catalyst development, offering resource-efficient and precise alternatives to conventional techniques. [15] [16]

7.2 Integration with Renewable Energy Systems for Sustainability

Electrochemical biomass conversion systems are increasingly being paired with renewable energy sources like solar and wind to enhance sustainability. For instance, solar-driven electrochemical setups have demonstrated the ability to convert bio-oil into hydrogen and methane with minimal energy input. These systems use carbon-based electrodes that efficiently store and utilize intermittent renewable energy for continuous operation. Advances in grid-independent systems have enabled decentralized processing, allowing small-scale biorefineries to integrate biomass conversion with local renewable energy sources, reducing transportation emissions and enhancing system efficiency. [15] [17]

Furthermore, hybrid energy systems combining photo-electrochemical and electro-biocatalytic pathways are emerging, leveraging both sunlight and biological activity for co-valorization of biomass and its byproducts. This dual-mode operation enhances overall efficiency and broadens the applicability of renewable-powered biomass conversion systems. [15] [16]

Figure 4 Biomass Cogeneration Schema

(CC BY-SA 4.0; adapted from Dcbert95, 2017; license details in ref.)

8 Conclusion and Perspectives

8.1 Summary of Advances in Carbon-Based Biomass Conversion

Significant advancements have been made in the development of carbon-based materials for electrochemical biomass conversion, emphasizing their sustainability and versatility. Biomass-derived carbons, such as nitrogen-doped graphene, hierarchical biochar, and carbon nanotube composites, have demonstrated remarkable performance in selective oxidation and reduction reactions. These materials exhibit high conductivity, chemical stability, and tunable surface functionalities, enabling efficient conversion of biomass intermediates like glycerol and 5-HMF into high-value products such as lactic acid and FDCA. Additionally, the integration of machine learning (ML) has accelerated the discovery and optimization of carbon materials tailored for specific biomass conversion pathways. This progress supports the deployment of these technologies at industrial scales, offering a renewable alternative to fossil-based processes while aligning with sustainability goals. [1] [3]

8.2 Challenges and Opportunities for Future Research

Despite these advances, challenges remain that hinder the widespread adoption of carbon-based biomass conversion technologies. These include:

- Durability and Scalability: Many carbon materials degrade under prolonged electrochemical operations, limiting their industrial viability.

- Selectivity and Yield: Achieving high selectivity for desired products without generating undesirable byproducts requires further tuning of catalyst properties.

- Economic Feasibility: While biomass-derived carbons are cost-effective compared to noble metals, scaling up production with consistent quality is a challenge.

Opportunities for Research:

- Advanced Functionalization: Research into novel doping strategies (e.g., dual-doping with nitrogen and sulphur) could enhance catalytic activity and selectivity.

- Hybrid Systems: Combining electrochemical processes with photochemical or biocatalytic pathways may broaden the range of biomass feedstocks and improve efficiency.

- Integration with Renewable Energy: Pairing electrochemical systems with solar or wind energy sources will further reduce the carbon footprint and operational costs, making these systems more attractive for large-scale applications [1] [3]

Future research should prioritize life-cycle assessments to quantify the environmental benefits of carbon-based biomass conversion systems and explore novel carbon materials derived from diverse biomass feedstocks to meet the rising global demand for sustainable energy and chemicals.

References

[1] Ruibo Fan, Beichen Xue, Pengfei Tian, Xuesong Zhang, Xiangzhou Yuan, and Huiyan Zhang, Sustainably transforming biomass into advanced carbon materials for solid-state supercapacitors, Chemical Communications, 2024. DOI: 10.1039/D4CC04762A.

[2]  Ziyi Fan, Wenjun Zhang, Liang Li, Yuqiao Wang, Yuqin Zou, Shungyin Wang, and Zupen Chen, Recent developments in electrode materials for the selective upgrade of biomass-derived platform molecules, Green Chemistry, 2022. DOI: 10.1039/D2GC02956A.

[3]  Guangying Zhang, Xu Liu, Lei Wang, and Honggang Fu, Recent advances of biomass-derived carbon-based materials for efficient electrochemical energy devices, Journal of Materials Chemistry A, 2023. DOI: 10.1039/D2TA01442D.

[4]  M. Pagliaro, R. Ciriminna, H. Kimura, Angewandte Chemie, Wiley Online Library, 2007. DOI: 10.1002/anie.200604694.

[5]  Shanqi Li, Shuangming Li, Yiwen Wang, Cheng Tang, Leilei Qiu, and Sansan Yu, Selective Oxidation of Glycerol to Lactic Acid Catalyzed by CuO/Activated Carbon and Reaction Kinetics, ACS Omega, 2024. DOI: 10.1021/acsomega.3c08845.

[6]  Yide-Rigen Bao, Yu Duan, and Yong Na, Electrochemical oxidation of 5-hydroxymethylfurfural to 2,5-furandicarboxylic acid catalyzed by bio-inspired NiMn layered double hydroxide, Journal of Materials Chemistry A, 2023. DOI: 10.1039/D3TA03408A.

[7]  Ting Sang, Hui Xu, Wenke Wang, Dongfang Ji, Jingcheng Hao, and Zhonghao Li, Platelike carbon-encapsulated nickel nanocrystals for efficient electrooxidation of 5-hydroxymethylfurfural, Chemical Communications, 2024. DOI: 10.1039/D4CC01443J.

[8]  Tianrui Song, Xianqiang Wang, Rui Guo, and Chang Liu, Recent advances in electrocatalytic oxidation of 5-HMF to FDCA by heterogeneous catalysts, Catalysts, 2024. DOI: 10.3390/catal14020157.

[9]  Enrique Guzmán-Mejía, Maria Torres-Martínez, and Carlos Alberto López-Ramírez, Thermochemical Production of Hydrogen from Biomass: Pyrolysis and Gasification, Energies, 2024, 17(2), 537. DOI: 10.3390/en17020537.

[10]  Michael A. Peters, Jacqueline K. Slaff, and Richard T. Williams, A Review of Current and Emerging Production Technologies for Biomass-Derived Sustainable Aviation Fuels, Energies, 2023, 16(16), 6100. DOI: 10.3390/en16166100.

[11]  Kore Infrastructure, Strategic Solutions for a Carbon-Negative, Zero-Waste Future. Retrieved 2024 from Kore Infrastructure.

[12]  Enrique Guzmán-Mejía, Maria Torres-Martínez, and Carlos Alberto López-Ramírez, Thermochemical Production of Hydrogen from Biomass: Pyrolysis and Gasification, Energies, 2024. DOI: 10.3390/en17020537.

[13]  Kai Wang, Yong Zhou, Xingchen Zhang, and Haining Liang, Electroreductive Upgradation of Biomass into High-Value Chemicals and Energy-Intensive Biofuels, Green Chemistry, 2024, 26, 2454-2475. DOI: 10.1039/D3GC04543A.

[14]  National Renewable Energy Laboratory (NREL), From Organics to Fuels: Computational Models Can Accelerate and Scale Up Biomass Conversion. Retrieved 2024 from NREL Website.

[15]  Nung Siong Lai, Kiara P. Nguyen, Matthew J. Krolczyk, and Emily J. Knight, An Artificial Intelligence (AI) workflow for catalyst design and optimization, Industrial & Engineering Chemistry Research, 2024, 62(43), 17835–17848. DOI: 10.48550/arXiv.2402.04557.

[16]  Johannes Jenewein, Lisa R. Müller, and Michael F. Barthel, Navigating the unknown with AI: multiobjective Bayesian optimization of non-noble acidic OER catalysts, Journal of Materials Chemistry A, 2024, 12, 3072-3083. DOI: 10.1039/D3TA06651G.

[17]  Sustainable Catalyst Design using AI/ML, ACS Green Chemistry Conference, 2023. DOI: www.gcande.org.

[18] ChemCatBio's work on electrocatalysis ChemCatBio.

[19] Ohio University's research on lignin electroconversion Ohio University.

[20] Overview articles on microbial and flow fuel cells ResearchGate.

[21] Fan, R., Xue, B., Tian, P., et al. Sustainably transforming biomass into advanced carbon materials for solid-state supercapacitors: a review. Chemical Communications, 2024. DOI:10.1039/D4CC04762A.

[22] Zhang, G., Liu, X., Wang, L., Fu, H. Recent advances of biomass-derived carbon-based materials for efficient electrochemical energy devices. Journal of Materials Chemistry A, 2022. DOI:10.1039/D2TA01442D.

[23] Zhu, P., et al. (2024). Electrocatalytic conversion of biomass-derived furan compounds: mechanisms, catalysts and perspectives. Chemical Science. DOI: 10.1039/D4SC00546E.

[24] Ruibo Fan et al., 2024. Sustainably transforming biomass into advanced carbon materials for solid-state supercapacitors. Chemical Communications. DOI: 10.1039/D4CC04762A.

[25] Enrique Guzmán-Mejía et al., 2024. Thermochemical Production of Hydrogen from Biomass: Pyrolysis and Gasification. Energies, 17(2), 537. DOI: 10.3390/en17020537.

[26] Guangying Zhang et al., 2023. Recent advances of biomass-derived carbon-based materials for efficient electrochemical energy devices. Journal of Materials Chemistry A. DOI: 10.1039/D2TA01442D.

[27] Peters, M. A., et al., 2023. A Review of Current and Emerging Production Technologies for Biomass-Derived Sustainable Aviation Fuels. Energies, 16(16), 6100. DOI: 10.3390/en16166100.

[28] Tian, C. et al. (2024). Progress and roadmap for electro-privileged transformations of bio-derived molecules. Nature Catalysis, 7(4), 350–360. DOI: 10.1038/s41929-024-01131-6.

[29] Yunfei Zhang & Yi Shen (2024). Electrochemical hydrogenation of levulinic acid, furfural and 5-hydroxymethylfurfural. Applied Catalysis B: Environmental, 343, 123576. DOI: 10.1016/j.apcatb.2023.123576.

[30] Qi, Y. et al. (2024). Recent advances in the electrocatalytic oxidative upgrading of lignocellulosic biomass. ChemPhysMater, 3(2), 157–186. DOI: 10.1016/j.chphma.2024.02.001.

[31] Yang, S. et al. (2025). Electrocatalytic oxidation of HMF to FDCA over multivalent ruthenium in neutral electrolyte. Molecules, 30(8), 1780. DOI: 10.3390/molecules30081780.

Figure 1: Cmx (2005). Electrochemical element with salt bridge, CC-BY SA 3.0

Figure 2: Vinay Bhat (2019). Review—Biomass Derived Carbon Materials for Electrochemical Sensors, CC‑BY 4.0

Figure 3: Onfray, C.; Thiam, A. Biomass-Derived Carbon-Based Electrodes for Electrochemical Sensing: A Review, Micromachines, 2023, 14(9), 1688. MDPI. Licensed under CC BY 4.0

Figure 4: Dcbert95 (2017). Biomass Cogeneration Schema, CC BY-SA 4.0

Abbreviations List

| Acronym | Full Form |
| --- | --- |
| HMF | 5-Hydroxymethylfurfural |
| FDCA | 2,5-Furandicarboxylic Acid |
| PEF | Polyethylene Furanoate |
| PET | Polyethylene Terephthalate |
| HER | Hydrogen Evolution Reaction |
| BDO | 2,3-Butanediol |
| RNG | Renewable Natural Gas |
| NREL | National Renewable Energy Laboratory |
| AI | Artificial Intelligence |
| ML | Machine Learning |
| LLM | Large Language Model |
| OER | Oxygen Evolution Reaction |
| MFC | Microbial Fuel Cell |